## Slide 1: Analysis of transfer learning to transfer process knowledge when processing different materials
Weibo Zhao, B. Sc.
Supervisor: Yannik Lockner, M. Sc.
13.10.2020
Notes: 站得稳一点，不要走
Good afternoon everyone, welcome to my master thesis presentation. My name is Weibo Zhao. I want to thank my supervisor Yannik Lockner for his help and guidance. The topic of my thesis is analysis of transfer learning to transfer process knowledge when processing different materials.
用左手拿笔
站得稳一点，不要走
Good afternoon everyone, welcome to my master thesis presentation. My name is Weibo Zhao. I want to thank my supervisor Yannik Lockner for his help and guidance. The topic of my thesis is analysis of transfer learning to transfer process knowledge when processing different materials.

## Slide 2: Outline
Motivation of applying transfer learning
Dataset description and feature ranking
Construction of DNN-ETL model
Transfer performance analysis
Application scenario of DNN-ETL
Conclusion and outlook
1
[URL00]
Notes: The presentation is divided into six parts.

## Slide 3: Outline
Motivation of applying transfer learning
Dataset description and feature ranking
Construction of DNN-ETL model
Transfer performance analysis
Application scenario of DNN-ETL
Conclusion and outlook
1
[URL00]
Notes: The first part is the motivation of applying transfer learning

## Slide 4: Motivation of applying transfer learning in injection molding Conventional deep learning approach
Objective
To analyse the possibility to transfer knowledge between processes where different materials are being utilized.
2
Notes: The objective of this thesis is to analyse the possibility to transfer knowledge between processes where different materials are being utilized. As for a conventional deep learning approach, we build a deep neural network, which is abbreviated as DNN. The input of this model are machine settings and material properties. And the output is the product quality values. We hope improve the prediction performance as much as possible. However, this approach faces two challenges: On the one hand, it requires large ﻿amount of process data to train the models, but in real-world applications, collecting injection molding data is a costly and time-consuming process. On the other hand, there is high training effort of the fitting models in the changes of production process. For example, when we change the product material, the DNN needs to rebuild from scratch. These challenges can be addressed by fostering transfer learning.

## Slide 5: Motivation of applying transfer learning in injection molding Conventional deep learning approach
Objective
To analyse the possibility to transfer knowledge between processes where different materials are being utilized.
Machine
settings
Product quality
Material properties
Deep Neural Network(DNN)
2
Notes: The objective of this thesis is to analyse the possibility to transfer knowledge between processes where different materials are being utilized. As for a conventional deep learning approach, we build a deep neural network, which is abbreviated as DNN. The input of this model are machine settings and material properties. And the output is the product quality values. We hope improve the prediction performance as much as possible. However, this approach faces two challenges: On the one hand, it requires large ﻿amount of process data to train the models, but in real-world applications, collecting injection molding data is a costly and time-consuming process. On the other hand, there is high training effort of the fitting models in the changes of production process. For example, when we change the product material, the DNN needs to rebuild from scratch. These challenges can be addressed by fostering transfer learning.

## Slide 6: Motivation of applying transfer learning in injection molding Conventional deep learning approach
Objective
To analyse the possibility to transfer knowledge between processes where different materials are being utilized.
Machine
settings
Product quality
Challenges
Require large ﻿amount of process data
High training effort of the fitting models in the changes of production process
Material properties
Deep Neural Network(DNN)
2
Notes: The objective of this thesis is to analyse the possibility to transfer knowledge between processes where different materials are being utilized. As for a conventional deep learning approach, we build a deep neural network, which is abbreviated as DNN. The input of this model are machine settings and material properties. And the output is the product quality values. We hope improve the prediction performance as much as possible. However, this approach faces two challenges: On the one hand, it requires large ﻿amount of process data to train the models, but in real-world applications, collecting injection molding data is a costly and time-consuming process. On the other hand, there is high training effort of the fitting models in the changes of production process. For example, when we change the product material, the DNN needs to rebuild from scratch. These challenges can be addressed by fostering transfer learning.

## Slide 7: Conducting experiments with a new material
Source dataset
Target dataset
Large process databank of multiple materials
Several data points of a new material
3

## Slide 8: Conducting experiments with a new material
Source dataset
Target dataset
Related but different
Same feature space
Different distribution
Large process databank of multiple materials
Several data points of a new material
3

## Slide 9: Comparison of conventional DNN and DNN with transfer learning
Source dataset
Learning system
source task
Conventional DNN
Target dataset
Learning system
target task
Training is isolated
Knowledge is not retained or accumulated
Source dataset
Learning system
source task
DNN-TL
Target dataset
Learning system
target task
Training of a new task relies on the previous learned task
Faster training, accurate, less training data
Knowledge
[OBL14]
4

## Slide 10: Outline
Motivation of applying transfer learning
Dataset description and feature ranking
Construction of DNN-ETL model
Transfer performance analysis
Application scenario of DNN-ETL
Conclusion and outlook
5
[URL00]
Notes: The second part is dataset description and feature ranking.

## Slide 11: Material series, polymer classes, manufacturers and amount
01
APEC
Polycarbonate
Company: Covestro
Amount: 13
02
PLEXIGLAS
Polymethylmethacrylat
Company: Evonik
Amount: 10
03
ULTRAMID
Polyamid
Company: BASF
Amount: 9
04
VALOX
Polybutylenterephthalat
Company: Sabic
Amount: 4
05
ULTEM
Polyetherimid
Company: Sabic
Amount: 6
06
SABIC PP
Polypropylene
Company: Sabic
Amount: 17
01
02
03
04
05
06
6
[URL01]
不要说数量
Notes: materials belong to different material series and also produced by different manufacturers.
APEC: Heat resistance in the secondary production process of smart devices.

## Slide 12
Input and output variables of DNN model based on injection moulding simulation
7
5 quality values:
 Part weight [g]
 Length [mm]
 Height [mm]
 Width [mm]
 Angle [°]
220 material properties:
 Solid density [kg/m3]
 Melt density [kg/m3]
 Thermal conductivity [ ]
……
6 machine settings:
Holding pressure. [bar]
Holding pressure time [s]
Melt temperature []
Cavity wall temperature []
Cooling time [s]
Injection flow rate [cm³/s]
Length
Height
Width
W°
Angle
Toy building block with 42 studs
60 materials, 77 experiments for each one
[Hei17]
Notes: We simulate the injection molding process of a toy building block with 4x2 studs in a software CADMOULD 10. We apply the simulation for 60 materials. 77 experiments of different process conditions are used for each of the material.There are 6 machine settings feature and 44 material properties features as the input of DNN model. The output are 5 quality values.
The total dataset contains two kinds of features:
Machine setting features: For each part, six machine setting parameters of the process are varied, namely holding pressure level, holding pressure time, mould temperature, cooling time, melt temperature, and volume ﬂow in a central composite experimental design with 77 test points.
Material property features: For totally 60 different materials, there are 138 physical, chemical, electronic, thermodynamic, and mechanical properties for each material. The dataset is exported from CADMould database.
The total dataset also includes five product quality values to measure the product quality.

## Slide 13
Input and output variables of DNN model based on injection moulding simulation
7
5 quality values:
 Part weight [g]
 Length [mm]
 Height [mm]
 Width [mm]
 Angle [°]
220 material properties:
 Solid density [kg/m3]
 Melt density [kg/m3]
 Thermal conductivity [ ]
……
6 machine settings:
Holding pressure. [bar]
Holding pressure time [s]
Melt temperature []
Cavity wall temperature []
Cooling time [s]
Injection flow rate [cm³/s]
Length
Height
Width
W°
Angle
Toy building block with 42 studs
60 materials, 77 experiments for each one
Some features are not related
[Hei17]
Notes: We simulate the injection molding process of a toy building block with 4x2 studs in a software CADMOULD 10. We apply the simulation for 60 materials. 77 experiments of different process conditions are used for each of the material.There are 6 machine settings feature and 44 material properties features as the input of DNN model. The output are 5 quality values.
The total dataset contains two kinds of features:
Machine setting features: For each part, six machine setting parameters of the process are varied, namely holding pressure level, holding pressure time, mould temperature, cooling time, melt temperature, and volume ﬂow in a central composite experimental design with 77 test points.
Material property features: For totally 60 different materials, there are 138 physical, chemical, electronic, thermodynamic, and mechanical properties for each material. The dataset is exported from CADMould database.
The total dataset also includes five product quality values to measure the product quality.

## Slide 14
Input and output variables of DNN model based on injection moulding simulation
7
5 quality values:
 Part weight [g]
 Length [mm]
 Height [mm]
 Width [mm]
 Angle [°]
220 material properties:
 Solid density [kg/m3]
 Melt density [kg/m3]
 Thermal conductivity [ ]
……
6 machine settings:
Holding pressure. [bar]
Holding pressure time [s]
Melt temperature []
Cavity wall temperature []
Cooling time [s]
Injection flow rate [cm³/s]
Length
Height
Width
W°
Angle
Toy building block with 42 studs
60 materials, 77 experiments for each one
Some features are not related
Apply feature ranking method
[Hei17]
Notes: We simulate the injection molding process of a toy building block with 4x2 studs in a software CADMOULD 10. We apply the simulation for 60 materials. 77 experiments of different process conditions are used for each of the material.There are 6 machine settings feature and 44 material properties features as the input of DNN model. The output are 5 quality values.
The total dataset contains two kinds of features:
Machine setting features: For each part, six machine setting parameters of the process are varied, namely holding pressure level, holding pressure time, mould temperature, cooling time, melt temperature, and volume ﬂow in a central composite experimental design with 77 test points.
Material property features: For totally 60 different materials, there are 138 physical, chemical, electronic, thermodynamic, and mechanical properties for each material. The dataset is exported from CADMould database.
The total dataset also includes five product quality values to measure the product quality.

## Slide 15: Feature importance score ranking for prediction of part weight
8
Chart: Feature importance [-]
| Solid density | Holding pressure | Thermal Conductivity | No Flow Temp | Ejection Temp | P2 | Melt density | N0 - Nu Polynom | Thermal diffusivity | Melt temperature | Melt Volume Rate | Suggested Mold Temp | Minimum Mold Temp | Pm4 | Injection flow rate | Maximum Mold Temp | Ts | Specific Heat | Melt Volume Rate | P3 | Cavity wall temperature | Cooling time | P1 | Pm1 | Pm2
 | 0.21539 | 0.12292 | 0.12057 | 0.1053 | 0.07396 | 0.046311 | 0.044874 | 0.034297 | 0.020239 | 0.01904 | 0.019033 | 0.018274 | 0.016138 | 0.011713 | 0.010976 | 0.010604 | 0.009182 | 0.008208 | 0.007636 | 0.007405 | 0.006941 | 0.006358 | 0.006318 | 0.005196 | 0.004288
Features [-]
Notes: Table 7.5 ranks the five features with the highest mean feature importance score of six feature ranking algorithms. Due to the space of the thesis, the rest features refer to the appendix.
For the overview of the whole features, Figure 7.4 illustrates the mean feature importance of each feature. The question now is to explain why some features are more important.

## Slide 16: Feature importance score ranking for prediction of part weight
8
Chart: Feature importance [-]
| Solid density | Holding pressure | Thermal Conductivity | No Flow Temp | Ejection Temp | P2 | Melt density | N0 - Nu Polynom | Thermal diffusivity | Melt temperature | Melt Volume Rate | Suggested Mold Temp | Minimum Mold Temp | Pm4 | Injection flow rate | Maximum Mold Temp | Ts | Specific Heat | Melt Volume Rate | P3 | Cavity wall temperature | Cooling time | P1 | Pm1 | Pm2
 | 0.21539 | 0.12292 | 0.12057 | 0.1053 | 0.07396 | 0.046311 | 0.044874 | 0.034297 | 0.020239 | 0.01904 | 0.019033 | 0.018274 | 0.016138 | 0.011713 | 0.010976 | 0.010604 | 0.009182 | 0.008208 | 0.007636 | 0.007405 | 0.006941 | 0.006358 | 0.006318 | 0.005196 | 0.004288
Features [-]
Delete the features with score lower than 10-5
44 material properties and 6 machine settings left
20 features are shown in this figure due to space
Notes: Table 7.5 ranks the five features with the highest mean feature importance score of six feature ranking algorithms. Due to the space of the thesis, the rest features refer to the appendix.
For the overview of the whole features, Figure 7.4 illustrates the mean feature importance of each feature. The question now is to explain why some features are more important.

## Slide 17: Feature importance score ranking for prediction of part weight
8
Chart: Feature importance [-]
| Solid density | Holding pressure | Thermal Conductivity | No Flow Temp | Ejection Temp | P2 | Melt density | N0 - Nu Polynom | Thermal diffusivity | Melt temperature | Melt Volume Rate | Suggested Mold Temp | Minimum Mold Temp | Pm4 | Injection flow rate | Maximum Mold Temp | Ts | Specific Heat | Melt Volume Rate | P3 | Cavity wall temperature | Cooling time | P1 | Pm1 | Pm2
 | 0.21539 | 0.12292 | 0.12057 | 0.1053 | 0.07396 | 0.046311 | 0.044874 | 0.034297 | 0.020239 | 0.01904 | 0.019033 | 0.018274 | 0.016138 | 0.011713 | 0.010976 | 0.010604 | 0.009182 | 0.008208 | 0.007636 | 0.007405 | 0.006941 | 0.006358 | 0.006318 | 0.005196 | 0.004288
Features [-]
5 features with highest feature importance
Notes: Table 7.5 ranks the five features with the highest mean feature importance score of six feature ranking algorithms. Due to the space of the thesis, the rest features refer to the appendix.
For the overview of the whole features, Figure 7.4 illustrates the mean feature importance of each feature. The question now is to explain why some features are more important.

## Slide 18: Analysis of 5 important influence factors
Solid density
Holding pressure
Thermal conductivity
No flow temperature
Ejection temperature
Product quality
Packing molecules together
in an orderly fashion
Shrinkage compensation
Related to part weight
Material stops flowing below certain temp.
Defining the amount of entering material
Influence shrinkage
Temperature distribution
Warpage of the mould
9
Notes: Product quality like part weight in the injection moulding process can be attributed to a wide variety of possible causes from material properties and machine setting parameters.
Holding pressure is used to finish filling the mould by packing the molecules together in an orderly fashion. After the mold cavity is filled, holding pressure is applied to compensate for shrinkage caused by cooling.
No flow temperature assumes that the polymer material stops flowing under processing condition below certain temperature. It defines the amount of material that enters into the cavity.
Ejection temperature is the temperature at which molded parts are ejected from the injection molding machine.
Thermal conductivity, which describes the heat conducting ability of the interface between a polymer and cavity wall, significantly influences the temperature distribution of a polymer and mould during injection moulding and thus affects the process and quality of plastic products.

## Slide 19: Summary of the dataset
6 machine settings
Product quality
44 material properties
Deep Neural Network(DNN)
10

## Slide 20: Outline
Motivation of applying transfer learning
Dataset description and feature ranking
Construction of DNN-ETL model
Transfer performance analysis
Application scenario of DNN-ETL
Conclusion and outlook
11
[URL00]

## Slide 21: Structure of deep neural network (DNN)
DNN after hyperparameter tuning
Pre-train on source task
 |  | …………………….. |  | 
 |  | …………………….. |  | 
 |  | …….. |  | 
 | …….. | 
Input layer
(50 node)
Hidden layer
(50 node)
Hidden layer
(25 node)
Hidden layer
(10 node)
Output layer
(5 node)
12
Knowledge:
DNN structure
Weights
Hyperparameters
…
Notes: Figure 8.1 illustrates the process of transferring the learned weights from the pre-trained model to the DNN-TL model.
Step 1: Pre-train model on the source dataset.
The workflow begins with a source dataset that consisted of data ﻿from five materials. This large source dataset is used to pre-train five DNN models from scratch.
﻿Step 2: Re-train the pre-trained model on the target dataset.
In this step, the weights learned by a pre-trained DNN model are transferred to a DNN-TL model

## Slide 22: Structure of DNN with transfer learning (DNN-TL)
DNN after hyperparameter tuning
Pre-train on source task
DNN-TL
Re-train on target task
 |  | …………………….. |  | 
 |  | …………………….. |  | 
 |  | …….. |  | 
 | …….. | 
 |  | …………………….. |  | 
 |  | …………………….. |  | 
 |  | …….. |  | 
 | …….. | 
Input layer
(50 node)
Hidden layer
(50 node)
Hidden layer
(25 node)
Hidden layer
(10 node)
Output layer
(5 node)
Knowledge reuse
12
Transfer knowledge from one model to another model
Notes: Figure 8.1 illustrates the process of transferring the learned weights from the pre-trained model to the DNN-TL model.
Step 1: Pre-train model on the source dataset.
The workflow begins with a source dataset that consisted of data ﻿from five materials. This large source dataset is used to pre-train five DNN models from scratch.
﻿Step 2: Re-train the pre-trained model on the target dataset.
In this step, the weights learned by a pre-trained DNN model are transferred to a DNN-TL model

## Slide 23: Structure of DNN with transfer and ensemble learning (DNN-ETL)
Input
5 Pre-trained DNN
Source dataset
Material properties
Machine settings
…
SABIC PP
VALOX
ULTEM
13
Notes: After the transfer learning step, 5 individual DNN-TL models are created by transferring the learned parameters from 5 DNN models. Then the deep neural network with ensemble learning and transfer learning (DNN-ETL) model is constructed. The overall structure of the proposed DNN-ETL is illustrated in Figure 8.5.

## Slide 24: Structure of DNN with transfer and ensemble learning (DNN-ETL)
Input
5 Pre-trained DNN
Source dataset
Material properties
Machine settings
…
SABIC PP
VALOX
ULTEM
13
5 material classes are selected as source dataset
Pre-train a DNN model on each of the material class
Notes: After the transfer learning step, 5 individual DNN-TL models are created by transferring the learned parameters from 5 DNN models. Then the deep neural network with ensemble learning and transfer learning (DNN-ETL) model is constructed. The overall structure of the proposed DNN-ETL is illustrated in Figure 8.5.

## Slide 25: Structure of DNN with transfer and ensemble learning (DNN-ETL)
DNN-TL
Target dataset
Input
5 Pre-trained DNN
Source dataset
Material properties
Machine settings
…
…
SABIC PP
VALOX
ULTEM
APEC
APEC
APEC
13
APEC dataset are selected as target dataset
Transfer knowledge from five models to one model
Notes: After the transfer learning step, 5 individual DNN-TL models are created by transferring the learned parameters from 5 DNN models. Then the deep neural network with ensemble learning and transfer learning (DNN-ETL) model is constructed. The overall structure of the proposed DNN-ETL is illustrated in Figure 8.5.

## Slide 26: Structure of DNN with transfer and ensemble learning (DNN-ETL)
DNN-TL
Target dataset
Input
5 Pre-trained DNN
Source dataset
Output of DNN-TL
Material properties
Machine settings
…
…
SABIC PP
VALOX
ULTEM
APEC
APEC
APEC
Fine tuning
Fine tuning
Fine tuning
…
Mean prediction
Quality value
Ensemble learning
DNN-ETL result
13
Notes: After the transfer learning step, 5 individual DNN-TL models are created by transferring the learned parameters from 5 DNN models. Then the deep neural network with ensemble learning and transfer learning (DNN-ETL) model is constructed. The overall structure of the proposed DNN-ETL is illustrated in Figure 8.5.

## Slide 27: Model comparison of R2 value
14
Algorithms [-]
Chart: 𝑅2 value for APEC dataset [-]
| Decision Tree | Random Forest | Gradient Boosting | Ada Boost | Extra Trees | XGBoost | Base DNN | DNN-EL | DNN-TL | DNN-ETL
 | 0.7339 | 0.6243 | 0.8287 | 0.6767 | 0.509 | 0.848 | 0.8707 | 0.8336 | 0.8934 | 0.9115
Base DNN: without transfer and ensemble
DNN-EL: with ensemble learning
DNN-TL: with transfer learning
DNN-ETL: with both transfer and ensemble
Notes: Firstly, based on the overall R2, the performance of the DNN-ETL method is better than that of other methods. The results suggest that the DNN-ETL method is capable of making more accurate quality estimations compared with the other considered methods. The mean absolute error of DNN-ETL is lower than the corresponding error of the other methods, which indicates that the overall performance of DNN-ETL is better than that of the other methods.
Secondly, the DNN-ETL model produces a R2 of 0.9207, which indicates that the proposed method can provide accurate quality estimations even if trained on a relatively small dataset. When comparing with the R2 of DNN-TL and DNN-EL, it can be concluded that both transfer learning and ensemble learning contribute to the capability of the DNN-ETL model to make accurate quality estimations.
Thirdly, the overall performance of all deep learning methods except DNN-EL is better than that of traditional machine learning methods. The slightly worse performance of DNN-EL in MAE metric can be explained by the use of a small target dataset, which might not provide sufficient training samples to make the complex DNN-EL model converge. Figure 8.6 visualises the performance of all the models as well as the derivations. The relative lower derivations of DNN-EL and DNN-ETL shows that ensemble learning helps to increase the robustness. Overall, the results suggest that deep learning methods can enable more accurate quality estimations compared to traditional machine learning methods such as Random Forest regression and Gradient Boosting regression.

## Slide 28: Model comparison of R2 value
14
Algorithms [-]
Chart: 𝑅2 value for APEC dataset [-]
| Decision Tree | Random Forest | Gradient Boosting | Ada Boost | Extra Trees | XGBoost | Base DNN | DNN-EL | DNN-TL | DNN-ETL
 | 0.7339 | 0.6243 | 0.8287 | 0.6767 | 0.509 | 0.848 | 0.8707 | 0.8336 | 0.8934 | 0.9115
Traditional machine learning
Deep learning
Notes: Firstly, based on the overall R2, the performance of the DNN-ETL method is better than that of other methods. The results suggest that the DNN-ETL method is capable of making more accurate quality estimations compared with the other considered methods. The mean absolute error of DNN-ETL is lower than the corresponding error of the other methods, which indicates that the overall performance of DNN-ETL is better than that of the other methods.
Secondly, the DNN-ETL model produces a R2 of 0.9207, which indicates that the proposed method can provide accurate quality estimations even if trained on a relatively small dataset. When comparing with the R2 of DNN-TL and DNN-EL, it can be concluded that both transfer learning and ensemble learning contribute to the capability of the DNN-ETL model to make accurate quality estimations.
Thirdly, the overall performance of all deep learning methods except DNN-EL is better than that of traditional machine learning methods. The slightly worse performance of DNN-EL in MAE metric can be explained by the use of a small target dataset, which might not provide sufficient training samples to make the complex DNN-EL model converge. Figure 8.6 visualises the performance of all the models as well as the derivations. The relative lower derivations of DNN-EL and DNN-ETL shows that ensemble learning helps to increase the robustness. Overall, the results suggest that deep learning methods can enable more accurate quality estimations compared to traditional machine learning methods such as Random Forest regression and Gradient Boosting regression.

## Slide 29: Model comparison of R2 value
14
Algorithms [-]
Chart: 𝑅2 value for APEC dataset [-]
| Decision Tree | Random Forest | Gradient Boosting | Ada Boost | Extra Trees | XGBoost | Base DNN | DNN-EL | DNN-TL | DNN-ETL
 | 0.7339 | 0.6243 | 0.8287 | 0.6767 | 0.509 | 0.848 | 0.8707 | 0.8336 | 0.8934 | 0.9115
Low standard deviation
Notes: Firstly, based on the overall R2, the performance of the DNN-ETL method is better than that of other methods. The results suggest that the DNN-ETL method is capable of making more accurate quality estimations compared with the other considered methods. The mean absolute error of DNN-ETL is lower than the corresponding error of the other methods, which indicates that the overall performance of DNN-ETL is better than that of the other methods.
Secondly, the DNN-ETL model produces a R2 of 0.9207, which indicates that the proposed method can provide accurate quality estimations even if trained on a relatively small dataset. When comparing with the R2 of DNN-TL and DNN-EL, it can be concluded that both transfer learning and ensemble learning contribute to the capability of the DNN-ETL model to make accurate quality estimations.
Thirdly, the overall performance of all deep learning methods except DNN-EL is better than that of traditional machine learning methods. The slightly worse performance of DNN-EL in MAE metric can be explained by the use of a small target dataset, which might not provide sufficient training samples to make the complex DNN-EL model converge. Figure 8.6 visualises the performance of all the models as well as the derivations. The relative lower derivations of DNN-EL and DNN-ETL shows that ensemble learning helps to increase the robustness. Overall, the results suggest that deep learning methods can enable more accurate quality estimations compared to traditional machine learning methods such as Random Forest regression and Gradient Boosting regression.

## Slide 30: Model comparison of R2 value
14
Algorithms [-]
Chart: 𝑅2 value for APEC dataset [-]
| Decision Tree | Random Forest | Gradient Boosting | Ada Boost | Extra Trees | XGBoost | Base DNN | DNN-EL | DNN-TL | DNN-ETL
 | 0.7339 | 0.6243 | 0.8287 | 0.6767 | 0.509 | 0.848 | 0.8707 | 0.8336 | 0.8934 | 0.9115
Better performance
High standard deviation
Notes: Firstly, based on the overall R2, the performance of the DNN-ETL method is better than that of other methods. The results suggest that the DNN-ETL method is capable of making more accurate quality estimations compared with the other considered methods. The mean absolute error of DNN-ETL is lower than the corresponding error of the other methods, which indicates that the overall performance of DNN-ETL is better than that of the other methods.
Secondly, the DNN-ETL model produces a R2 of 0.9207, which indicates that the proposed method can provide accurate quality estimations even if trained on a relatively small dataset. When comparing with the R2 of DNN-TL and DNN-EL, it can be concluded that both transfer learning and ensemble learning contribute to the capability of the DNN-ETL model to make accurate quality estimations.
Thirdly, the overall performance of all deep learning methods except DNN-EL is better than that of traditional machine learning methods. The slightly worse performance of DNN-EL in MAE metric can be explained by the use of a small target dataset, which might not provide sufficient training samples to make the complex DNN-EL model converge. Figure 8.6 visualises the performance of all the models as well as the derivations. The relative lower derivations of DNN-EL and DNN-ETL shows that ensemble learning helps to increase the robustness. Overall, the results suggest that deep learning methods can enable more accurate quality estimations compared to traditional machine learning methods such as Random Forest regression and Gradient Boosting regression.

## Slide 31: Model comparison of R2 value
Chart: 𝑅2 value for APEC dataset [-]
| Decision Tree | Random Forest | Gradient Boosting | Ada Boost | Extra Trees | XGBoost | Base DNN | DNN-EL | DNN-TL | DNN-ETL
 | 0.7339 | 0.6243 | 0.8287 | 0.6767 | 0.509 | 0.848 | 0.8707 | 0.8336 | 0.8934 | 0.9115
14
Algorithms [-]
Best performance 0.9207
Low standard deviation
Notes: Firstly, based on the overall R2, the performance of the DNN-ETL method is better than that of other methods. The results suggest that the DNN-ETL method is capable of making more accurate quality estimations compared with the other considered methods. The mean absolute error of DNN-ETL is lower than the corresponding error of the other methods, which indicates that the overall performance of DNN-ETL is better than that of the other methods.
Secondly, the DNN-ETL model produces a R2 of 0.9207, which indicates that the proposed method can provide accurate quality estimations even if trained on a relatively small dataset. When comparing with the R2 of DNN-TL and DNN-EL, it can be concluded that both transfer learning and ensemble learning contribute to the capability of the DNN-ETL model to make accurate quality estimations.
Thirdly, the overall performance of all deep learning methods except DNN-EL is better than that of traditional machine learning methods. The slightly worse performance of DNN-EL in MAE metric can be explained by the use of a small target dataset, which might not provide sufficient training samples to make the complex DNN-EL model converge. Figure 8.6 visualises the performance of all the models as well as the derivations. The relative lower derivations of DNN-EL and DNN-ETL shows that ensemble learning helps to increase the robustness. Overall, the results suggest that deep learning methods can enable more accurate quality estimations compared to traditional machine learning methods such as Random Forest regression and Gradient Boosting regression.

## Slide 32: Outline
Motivation of applying transfer learning
Dataset description and feature ranking
Construction of DNN-ETL model
Transfer learning performance analysis
Application scenario of DNN-ETL
Conclusion and outlook
15
[URL00]

## Slide 33
All materials
except APEC
Input A
APEC dataset
Input B
Output A
Output B
Base A
Base B
16
Experiment setup: scenario 1
[YCB+14]
1
Notes: A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. ) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].
A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. 𝑊_𝐴1) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer 𝑛 = 2 is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].

## Slide 34
All materials
except APEC
Input A
APEC dataset
Input B
Output A
Output B
Base A
Base B
16
Experiment setup: scenario 1
Weight vector
Layer
[YCB+14]
1
Notes: A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. ) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].
A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. 𝑊_𝐴1) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer 𝑛 = 2 is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].

## Slide 35
All materials
except APEC
Input A
APEC dataset
Input B
Output A
Output B
Base A
Transfer learning
frozen weights
17
Experiment setup: scenario 2
[YCB+14]
2
To simplify the model, we don’t consider ensemble learning
but mainly focus on transfer learning, namely DNN-TL model
Notes: A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. ) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].
A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. 𝑊_𝐴1) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer 𝑛 = 2 is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].

## Slide 36
All materials
except APEC
Input A
APEC dataset
Input B
Output A
Output B
Base A
Transfer learning
frozen weights
17
Experiment setup: scenario 2
[YCB+14]
2
Random initialised
Notes: A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. ) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].
A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. 𝑊_𝐴1) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer 𝑛 = 2 is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].

## Slide 37
All materials
except APEC
Input A
APEC dataset
Input B
Output A
Output B
Base A
Transfer learning
frozen weights
17
Experiment setup: scenario 2
[YCB+14]
2
Two layers are copied from Base A
Locked: weights are not trainable
Notes: A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. ) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].
A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. 𝑊_𝐴1) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer 𝑛 = 2 is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].

## Slide 38
All materials
except APEC
Input A
APEC dataset
Input B
Output A
Output B
Base A
Transfer learning
fine tuning
18
Experiment setup: scenario 3
[YCB+14]
3
Notes: A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. ) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].
A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. 𝑊_𝐴1) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer 𝑛 = 2 is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].

## Slide 39
All materials
except APEC
Input A
APEC dataset
Input B
Output A
Output B
Base A
Transfer learning
fine tuning
18
Experiment setup: scenario 3
[YCB+14]
3
Two layers are copied from Base A
Unlocked: weights are trainable
Notes: A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. ) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].
A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. 𝑊_𝐴1) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer 𝑛 = 2 is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].

## Slide 40
APEC dataset
Input B
Output B
Transfer learning
frozen weights
19
Experiment setup overview
All materials
except APEC
Input A
APEC dataset
Input B
Output A
Output B
Base A
Base B
APEC dataset
Input B
Output B
Transfer learning
fine tuning
1
2
3
[YCB+14]
Notes: A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. ) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].
A five-layer neural network is trained on A and another on B. These networks, which are called Base A and Base B, are shown in the top two rows of Figure 9.1. The labelled rectangles (e.g. 𝑊_𝐴1) represent the weight vector learned for that layer, with the colour indicating which dataset the layer was originally trained on. The vertical bars between weight vectors represent the activations of the network at each layer. A layer n is chosen to train several new networks. In the following explanation and in Figure 9.1, layer 𝑛 = 2 is used as the example layer chosen. The following two networks are defined and trained:
A self transfer network B2B: The first 2 layers are copied from Base B and frozen. The next layers are initialised randomly and trained on dataset B. This network is a control for the next transfer network.
A transfer learning network A2B: The first 2 layers are copied from Base A and frozen. The next layers are initialised randomly and trained toward dataset B. Intuitively, here the first 2 layers are copied from a network trained on dataset A and then learn higher layer features on top of them to predict on a new target dataset B. If A2B performs as well as Base B, there is evidence that the second-layer features are general, at least with respect to B. If performance suffers, there is evidence that the second-layer features are specific to A [YCB+14].

## Slide 41: Effect of the training dataset size on transfer learning
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Scenario 1: no transfer learning | 0.70558 | 0.8874 | 0.92225 | 0.91953 | 0.93167 | 0.90571 | 0.9076 | 0.90784 | 0.92487 | 0.92267
20
Notes: The results of this comparison and the effect of the training dataset size on R2 value are illustrated in Figure 9.4. ‘%’ in the sub-caption denotes availability of target domain data.
Firstly, it can be observed that the performance improvement of DNN-TL over DNN is attributed to employing transfer learning.

## Slide 42: Effect of the training dataset size on transfer learning
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Scenario 1: no transfer learning | 0.70558 | 0.8874 | 0.92225 | 0.91953 | 0.93167 | 0.90571 | 0.9076 | 0.90784 | 0.92487 | 0.92267
20
1001 samples for the total APEC training dataset
Notes: The results of this comparison and the effect of the training dataset size on R2 value are illustrated in Figure 9.4. ‘%’ in the sub-caption denotes availability of target domain data.
Firstly, it can be observed that the performance improvement of DNN-TL over DNN is attributed to employing transfer learning.

## Slide 43: Effect of the training dataset size on transfer learning
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Scenario 1: no transfer learning | 0.70558 | 0.8874 | 0.92225 | 0.91953 | 0.93167 | 0.90571 | 0.9076 | 0.90784 | 0.92487 | 0.92267
Scenario 2: transfer learning frozen weights | 0.71115 | 0.92785 | 0.95329 | 0.96469 | 0.96794 | 0.97234 | 0.96831 | 0.97528 | 0.96789 | 0.98472
20
Notes: The results of this comparison and the effect of the training dataset size on R2 value are illustrated in Figure 9.4. ‘%’ in the sub-caption denotes availability of target domain data.
Firstly, it can be observed that the performance improvement of DNN-TL over DNN is attributed to employing transfer learning.

## Slide 44: Effect of the training dataset size on transfer learning
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Scenario 1: no transfer learning | 0.70558 | 0.8874 | 0.92225 | 0.91953 | 0.93167 | 0.90571 | 0.9076 | 0.90784 | 0.92487 | 0.92267
Scenario 2: transfer learning frozen weights | 0.71115 | 0.92785 | 0.95329 | 0.96469 | 0.96794 | 0.97234 | 0.96831 | 0.97528 | 0.96789 | 0.98472
Scenario 3: transfer learning fine tuning | 0.98762 | 0.98211 | 0.98937 | 0.98696 | 0.98087 | 0.99092 | 0.98997 | 0.97923 | 0.98578 | 0.98557
20
Notes: The results of this comparison and the effect of the training dataset size on R2 value are illustrated in Figure 9.4. ‘%’ in the sub-caption denotes availability of target domain data.
Firstly, it can be observed that the performance improvement of DNN-TL over DNN is attributed to employing transfer learning.

## Slide 45: Effect of the training dataset size on transfer learning
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Scenario 1: no transfer learning | 0.70558 | 0.8874 | 0.92225 | 0.91953 | 0.93167 | 0.90571 | 0.9076 | 0.90784 | 0.92487 | 0.92267
Scenario 2: transfer learning frozen weights | 0.71115 | 0.92785 | 0.95329 | 0.96469 | 0.96794 | 0.97234 | 0.96831 | 0.97528 | 0.96789 | 0.98472
Scenario 3: transfer learning fine tuning | 0.98762 | 0.98211 | 0.98937 | 0.98696 | 0.98087 | 0.99092 | 0.98997 | 0.97923 | 0.98578 | 0.98557
20
Notes: The results of this comparison and the effect of the training dataset size on R2 value are illustrated in Figure 9.4. ‘%’ in the sub-caption denotes availability of target domain data.
Firstly, it can be observed that the performance improvement of DNN-TL over DNN is attributed to employing transfer learning.

## Slide 46: Effect of the training dataset size on transfer learning
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Scenario 1: no transfer learning | 0.70558 | 0.8874 | 0.92225 | 0.91953 | 0.93167 | 0.90571 | 0.9076 | 0.90784 | 0.92487 | 0.92267
Scenario 2: transfer learning frozen weights | 0.71115 | 0.92785 | 0.95329 | 0.96469 | 0.96794 | 0.97234 | 0.96831 | 0.97528 | 0.96789 | 0.98472
Scenario 3: transfer learning fine tuning | 0.98762 | 0.98211 | 0.98937 | 0.98696 | 0.98087 | 0.99092 | 0.98997 | 0.97923 | 0.98578 | 0.98557
20
Transfer learning with fine tuning can achieve good performance based on very small dataset
Notes: The results of this comparison and the effect of the training dataset size on R2 value are illustrated in Figure 9.4. ‘%’ in the sub-caption denotes availability of target domain data.
Firstly, it can be observed that the performance improvement of DNN-TL over DNN is attributed to employing transfer learning.

## Slide 47: Effect of the training dataset size on transfer learning
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Scenario 1: no transfer learning | 0.70558 | 0.8874 | 0.92225 | 0.91953 | 0.93167 | 0.90571 | 0.9076 | 0.90784 | 0.92487 | 0.92267
Scenario 2: transfer learning frozen weights | 0.71115 | 0.92785 | 0.95329 | 0.96469 | 0.96794 | 0.97234 | 0.96831 | 0.97528 | 0.96789 | 0.98472
Scenario 3: transfer learning fine tuning | 0.98762 | 0.98211 | 0.98937 | 0.98696 | 0.98087 | 0.99092 | 0.98997 | 0.97923 | 0.98578 | 0.98557
20
Under similar performance,
transfer learning needs less data
Notes: The results of this comparison and the effect of the training dataset size on R2 value are illustrated in Figure 9.4. ‘%’ in the sub-caption denotes availability of target domain data.
Firstly, it can be observed that the performance improvement of DNN-TL over DNN is attributed to employing transfer learning.

## Slide 48: Effect of the training dataset size on transfer learning
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Scenario 1: no transfer learning | 0.70558 | 0.8874 | 0.92225 | 0.91953 | 0.93167 | 0.90571 | 0.9076 | 0.90784 | 0.92487 | 0.92267
Scenario 2: transfer learning frozen weights | 0.71115 | 0.92785 | 0.95329 | 0.96469 | 0.96794 | 0.97234 | 0.96831 | 0.97528 | 0.96789 | 0.98472
Scenario 3: transfer learning fine tuning | 0.98762 | 0.98211 | 0.98937 | 0.98696 | 0.98087 | 0.99092 | 0.98997 | 0.97923 | 0.98578 | 0.98557
20
Significant improvement
Notes: The results of this comparison and the effect of the training dataset size on R2 value are illustrated in Figure 9.4. ‘%’ in the sub-caption denotes availability of target domain data.
Firstly, it can be observed that the performance improvement of DNN-TL over DNN is attributed to employing transfer learning.

## Slide 49: Improvement percentage of R2 value due to transfer learning
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
﻿Average improvement | 28.5578 | 9.6437 | 6.7843 | 6.832 | 5.0154 | 8.5989 | 8.3205 | 7.2905 | 6.1783 | 6.382
21
Notes: The performance improvement becomes apparent as the training dataset size decreases, suggesting that transfer learning is a useful tool for enhancing the quality estimation performance, especially when the training dataset is small. As the size of the training dataset increases, the performance improvement results from employing transfer learning gradually decreased. This is because it is difficult to find parameters that can simultaneously fit the source and target tasks very well.

## Slide 50: Improvement percentage of R2 value due to transfer learning
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
﻿Average improvement | 28.5578 | 9.6437 | 6.7843 | 6.832 | 5.0154 | 8.5989 | 8.3205 | 7.2905 | 6.1783 | 6.382
21
Average improvement of 9.36 %
Notes: The performance improvement becomes apparent as the training dataset size decreases, suggesting that transfer learning is a useful tool for enhancing the quality estimation performance, especially when the training dataset is small. As the size of the training dataset increases, the performance improvement results from employing transfer learning gradually decreased. This is because it is difficult to find parameters that can simultaneously fit the source and target tasks very well.

## Slide 51: Outline
Motivation of applying transfer learning
Dataset description and feature ranking
Construction of DNN-ETL model
Transfer learning performance analysis
Application scenario of DNN-ETL
Conclusion and outlook
22
[URL00]

## Slide 52: Application in finding best machine settings
23
[Hei17]
Machine operator
Machine settings
Trial of machine settings based on:
 Recommendations of material supplier
 Experience, intuition of the operator
Quality feedback
Product quality
e.g. target weight
Notes: The process towards an optimised machine parameter setting is recognized as one of the most important steps in injection moulding for improving the quality of moulded products [SWL07]. Since the quality of injection moulded plastic parts can be influenced by process conditions, how to determine the optimal machine setting parameters for different materials becomes the key to improving the part quality.

## Slide 53: Part weight prediction of random machine settings combination
Material properties
Machine settings
…
…
SABIC
VALOX
ULTEM
APEC
APEC
APEC
Fine tuned DNN
Fine tuned DNN
Fine tuned DNN
…
Mean prediction
Quality value
Proposed DNN-ETL model
Prediction result of 10000 samples
25
Blue points are output samples

## Slide 54: Output of process condition recommender system
Current machine setting parameters
No. | Melt temp. | Cavity temp. | Press time | Cool time | Flow rate | Hold press
1 | 245 | 48 | 1 | 1.5 | 43 | 490
Satisfactory points
(10 samples)
Example experiment
Target weight
26
Notes: Calculate distance from current state

## Slide 55: Output of process condition recommender system
Current machine setting parameters
No. | Melt temp. | Cavity temp. | Press time | Cool time | Flow rate | Hold press
1 | 245 | 48 | 1 | 1.5 | 43 | 490
No. | Melt temp. | Cavity temp. | Press time | Cool time | Flow rate | Hold press
1 | 246 | 67 | 0.2 | 1.8 | 32 | 480
2 | 249 | 64 | 0.2 | 2 | 49 | 610
3 | 245 | 42 | 0.7 | 2.4 | 44 | 480
10 | 245 | 55 | 1.1 | 1.9 | 53 | 600
No. | Melt temp. | Cavity temp. | Press time | Cool time | Flow rate | Hold press
1 | 246 | 67 | 0.2 | 1.8 | 32 | 480
2 | 249 | 64 | 0.2 | 2 | 49 | 610
3 | 245 | 42 | 0.7 | 2.4 | 44 | 480
10 | 245 | 55 | 1.1 | 1.9 | 53 | 600
Satisfactory points
(10 samples)
Example experiment
Target weight
Final recommend conditions
Calculate distance
26
Evaluation fuction
Notes: Calculate distance from current state

## Slide 56: Outline
Motivation of applying transfer learning
Dataset description and feature ranking
Construction of DNN-ETL model
Transfer learning performance analysis
Application scenario of DNN-ETL
Conclusion and outlook
27
[URL00]

## Slide 57: Conclusion and outlook
28
R² test score is 0.9207 and it surpasses the state-of-the-art performance of 0.90 [TGH+18]
Develop DNN-ETL model
An average improvement of 9.36 % of R² value can be achieved compared to DNN without transfer learning.
Analyse the improvement due to transfer learning
Five most important features: solid density, holding pressure, thermal conductivity, no flow temperature and ejection temperature
Apply feature ranking method

## Slide 58: Conclusion and outlook
28
Two datasets with same feature space
“when to transfer”
“what to transfer”
R² test score is 0.9207 and it surpasses the state-of-the-art performance of 0.90 [TGH+18]
Develop DNN-ETL model
An average improvement of 9.36 % of R² value can be achieved compared to DNN without transfer learning.
Analyse the improvement due to transfer learning
Five most important features: solid density, holding pressure, thermal conductivity, no flow temperature and ejection temperature
Apply feature ranking method

## Slide 59: Conclusion and outlook
R² test score is 0.9207 and it surpasses the state-of-the-art performance of 0.90 [TGH+18]
Develop DNN-ETL model
An average improvement of 9.36 % of R² value can be achieved compared to DNN without transfer learning.
Analyse the improvement due to transfer learning
Five most important features: solid density, holding pressure, thermal conductivity, no flow temperature and ejection temperature
Apply feature ranking method
28
Algorithms
Two datasets with same feature space
Test whether the marginal distributions
of two domains are similar

## Slide 60
I am happy to answer your questions.
Weibo Zhao Telefon: +49 1637640827 E-Mail: weibo.zhao@rwth-aachen.de
29

## Slide 61: References
30
[Hei17]: Heinisch, J.: From simulation to injection moulding machine - Optimized process setup based on machine learning citation. International Mold Conference Bucheon, 2017
[OBL14]: OQUAB, M.; BOTTOU, L.; LAPTEV, I.; SIVIC, J.: Learning and transferring mid-level image representations using convolutional neural networks. Proceedings of the IEEE conference on computer vision and pattern recognition, 1717-1724, 2014
[TGH+18]: TERCAN, H.; GUAJARDO, A.; HEINISCH, J.; THIELE, T., HOPMANN, C.; MEISEN, T.: Transfer-Learning: Bridging the Gap Between Real and Simulation Data for Machine Learning in Injection Moulding, Proc. CIRP,72, 185–190, 2018
[TS09]: TORREY, L.; SHAVLIK, J.: Transfer Learning. Handbook of Research on Machine Learning Applications. IGI Global, 2009
[URL00]: N.N.: Injection moulding machine, https://www.seasongroup.com/manufacturing-services/plastic-injection-molding/
[URL01]: N.N.: PLEXIGLAS Zuschnitt nach Maß. URL: https://kunststoffplattenonline.de/plexiglas/, 24.09.2020
[YCB+14]: YOSINSKI, J.; CLUNE, J.; BENGIO, Y.; LIPSON, H.: How transferable are features in deep neural networks? Conference of Advances in Neural Information Processing Systems. 3320-3328, 2014

## Slide 62: Data visualization of the part weight of the six material classes
Material class [-]
Part weight [g]
Figure 7.3
Notes: The 60 materials can be divided to six product classes, namely APEC, PLEXIGLAS, SABIC PP, ULTEM, ULTRAMID and VALOX. Figure 7.3 shows that the quality values like part weight within a same material class have similar range compared to other material classes. Each point represents a simulation result of one material under certain machine setting conditions. The part weight of the toy building block is influenced by the class of materials.

## Slide 63: Different part weight distribution of six material classes
Chart: Part weight [g]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Transfer on 2 sources | -0.65786 | 0.78867 | 0.91295 | 0.93855 | 0.93473 | 0.95444 | 0.947 | 0.96466 | 0.96437 | 0.97572
Transfer on 3 sources | 0.26902 | 0.65035 | 0.90728 | 0.91638 | 0.93412 | 0.9629 | 0.96164 | 0.95907 | 0.97552 | 0.97603
45 50 55 60 65 70 75
APEC
PLEXIGLAS
SABIC PP
ULTEM
ULTRAMID
VALOX
23
Cadmould simulations data
Use different dataset
Notes: The quality values of different material classes have different data distributions, shown in Figure 9.5. This justifies the need for multi-source transfer learning, where knowledge is transferred from each source database to the DNN-TL model. In the whole source dataset, each material class represents a source with its own distribution. It is interesting to investigate how the number of source data with different distributions affect the performance of DNN-TL on target task.

## Slide 64: Qualitative depiction of 2n-Experiment (n=3) plan including star and center point
Figure 7.2
×Step value
2 ×Step value
Central composite design
(CCD) of experiments:
77 times of Machine settings combination
Full-factorial experimental design (64-point cube) 26
Star points outside the cube (12 points)
Central point

## Slide 65: Feature ranking by ensemble learning method
Machine settings and material properties
Regression models/
Feature ranking methods
Predictions/
Feature importance score
Ensemble’s prediction
Ensemble regressor
1
2
3
4
5
6
Mean value
Decision
Tree
Random
Forest
Gradient
Boost
Ada
boost
Extra
Tree
XGBoost
Same dataset
8
可以用在both Predictions/
Feature importance
放在后面，如果有人问在拿出来
Notes: Feature ranking algorithms rank the features in accordance with their predictive scores. Six feature ranking techniques are applied, namely XGBoost [MHK20], Extra Tree [GEW06], Decision Tree [Loh11], Gradient Boosting [HTF09], Ada Boost [TLX17] and Random Forest [Bre01]. For each method, the features are ranked with the calculated feature importance score, the sum of which is equal to one. Due to different principle of algorithms, the feature ranking results of six methods differ from each other. One plausible solution is to use the ensemble learning idea to calculate the summation or mean importance score of each feature.

## Slide 66: Splitting source dataset into 5 folds according to material classes
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX | APEC
Total dataset
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX
Source task
APEC
Target task
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX
Pre-trained DNN 1
Pre-trained DNN 2
Pre-trained DNN 3
Pre-trained DNN 4
Pre-trained DNN 5
13
Notes: As illustrated in Figure 8.4, the APEC dataset is selected as target task, while the whole dataset of the rest material classes is the source task. In pre-training, the source dataset was first split into 5 folds according to the material classes. Subsequently, a fold of the data (indicated by the green block) is held out to pre-train a DNN model. As a result, 5 pre-trained DNN models are trained using the source dataset, each associated with one material.

## Slide 67: Possible advantages due to transfer learning
Chart: Amount of training set [-]
[TS09]
4
R2 value
Coefficient of determination
The higher, the better performance
Notes: From literature, there a three possible advantages due to transfer learning. The metric we use to evaluate the performance of the model is R2. The higher the value, the better the model performance. We compare the R2 value under different amount of training set. The green curve is the model with transfer learning while the black curve without transfer learing. It can be found that the green curve has higher start, higher slope and higher asymptote, which means transfer learning has better performance.

## Slide 68: Possible advantages due to transfer learning
Chart: Amount of training set [-]
[TS09]
4
3
Higher asymptote
2
Higher slope
1
Higher start
R2 value
Notes: From literature, there a three possible advantages due to transfer learning. The metric we use to evaluate the performance of the model is R2. The higher the value, the better the model performance. We compare the R2 value under different amount of training set. The green curve is the model with transfer learning while the black curve without transfer learing. It can be found that the green curve has higher start, higher slope and higher asymptote, which means transfer learning has better performance.

## Slide 69: Difference of frozen weights and fine tuning
All material
except APEC
Input A
19
Back propagation
Back propagation
AnB: Frozen weights
AnB+: Fine tuning
Transferred layer n
Forward direction
Output A
APEC dataset
Input B
Output B
[propagation
Notes: This process is repeated for all n. In the above two networks, the transferred layers are frozen. There are two versions of the above two networks where the transferred layers are fine-tuned:
A self transfer network B2B+: just like B2B, but where all layers learn.
A transfer network A2B+: just like A2B, but where all layers learn.
Figure 9.2 depicts the difference between frozen weights and fine tuning.

## Slide 70: Generation of input features
Melt temperature
245 Step 1 270
Cavity wall temperature
40 Step 1 100
Holding pressure time
0.2 Step 0.1 1.2
Cooling time
1.5 Step 0.1 2.5
Injection flow rate
30 Step 1 55
Holding pressure
400 Step 10 912
Material properties
extracted from mould
Machine settings
+
24
10000 samples with random machine settings
Notes: The process towards an optimised machine parameter setting is recognized as one of the most important steps in injection moulding for improving the quality of moulded products [SWL07]. Since the quality of injection moulded plastic parts can be influenced by process conditions, how to determine the optimal machine setting parameters for different materials becomes the key to improving the part quality.

## Slide 71: Thesis figures

## Slide 72: Mögliche Vorteile durch Transferlernen
Chart: ﻿Trainingsumfang
[TS09]
Abbildung 2.1
3
Höhere Asymptote
2
Höhere Steigung
1
Höherer Start
ohne Transferlernen
mit Transferlernen

## Slide 73: Verbesserung des R2-Werts durch Transferlernen bei Vorhandensein weniger Daten der APEC-Materialdomäne
Chart: ﻿Trainingsdatenanteil am Gesamtdatensatz [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
﻿Average improvement | 28.5578 | 9.6437 | 6.7843 | 6.832 | 5.0154 | 8.5989 | 8.3205 | 7.2905 | 6.1783 | 6.382
Abbildung 2.2
﻿Durchschnittliche Verbesserung

## Slide 74: Possible advantages due to transfer learning
Chart: Amount of training
[TS09]
Figure 2.1
3
Higher asymptote
2
Higher slope
1
Higher start

## Slide 75: Improvement of the R2 value by transfer learning in presence of few data from the APEC material domain
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
﻿Average improvement | 28.5578 | 9.6437 | 6.7843 | 6.832 | 5.0154 | 8.5989 | 8.3205 | 7.2905 | 6.1783 | 6.382
Figure 2.2

## Slide 76: Research methodology approach
Simulation
Data mining
Raw dataset
Data visualization
Preprocessing
Model construction
Feature ranking
Deep learning
Transfer learning
Ensemble learning
Weight frozen / fine tuning
Training data size
Number of transferred layers
Single or multisource transfer
Single task and multitask learning
Traditional machine learning
Comparison
Figure 3.1

## Slide 77: Depiction of an injection moulding machine
[Kra05]
Figure 4.1
Notes: Schematics of the IM machine can be seen in figure
Kramschuster, A., et al., Quantitative study of shrinkage and warpage behavior for microcellular and conventional injection molding, Polym. Eng. Sci., (2005) 45(10): pp. 1408–1418

## Slide 78: Influence factors of product quality in injection moulding
Tolerance ____
Symmetry_???
Ribs design_?_
Reinforcement__
Wall dimensions_
Part design
Man
Environment
Mold design
Material
Machine setting
Holding pressure time
Cavity wall temperature_
Melt temperature__
Holding pressure___
Injection flow rate____
Cooling time_____
Specific heat constant
Thermal conductivity_
Thermal diffusivity__
Solid density___
Melt density____
E constant_____
Cooling channel
Venting holes_
Flow design__
Injection type___
Runner____
Gates_____
_____
Training_???
Experience_?_
Supervision__
Air currents____
Relative humidity ???
Ambient temperature_?_
Cooling water temp.__
Interface conditions _
Product quality
[STT+08]
Figure 4.2
Notes: Injection moulding is a complex process, from design, fabrication, assembly, testing, and finally being put into use. Throughout the life cycle, there are many factors affecting injection moulding quality from all kind of aspects of raw material properties, mould design, injection moulding machine setting and so on. A better control of these influence factors allows for a better final quality of the injection moulding products.

## Slide 79: Process setup by means of machine learning
Figure 4.3
Design of experiments
Injection moulding simulation
Model construction
Optimisation

## Slide 80: A practical view of a machine learning system
Figure 5.1
Training
Predicting
Raw data
Feature
engineering
Training
set
Validation
set
Test
set
Machine
learning
Model
New data
Feature
engineering
Prediction
Target
Model training
Model selection
Evaluation
[Osm19]
Notes: https://techblog.cdiscount.com/assets/images/DataScience/automl/ML_process.png[Osm19]

## Slide 81
Methods of machine learning
Machine
learning
Supervised
learning
Unsupervised
learning
Classification Regression Clustering
 Logistic
regressions
 Support Vector Machines
 Random forest
 Extra tree
 Decision tree
 Deep neural networks
 Connectivity- based clustering
 Distribution- based clustering
Figure 5.2
[Mit97]

## Slide 82: Model performance influenced by number of training epohcs
Underfitting
Overfitting
Error
Training error
Generalization error
Number of training epochs
Just right
Early stopping
Figure 5.3
[GBC16]

## Slide 83: Comparison of underfitting, appropriate fitting and overfitting
Figure 5.4
[FW95]
Underfitting
(Too simple to explain the variance)
Appropriate fitting
(Good Generalization)
Overfitting
(Too good to be true)

## Slide 84: Cross validation
Figure 5.5
Cross validation
Total dataset
Fold 1 | Fold 2 | Fold 3 | Fold 4 | Fold 5
Fold 1 | Fold 2 | Fold 3 | Fold 4 | Fold 5
Fold 1 | Fold 2 | Fold 3 | Fold 4 | Fold 5
Fold 1 | Fold 2 | Fold 3 | Fold 4 | Fold 5
Fold 1 | Fold 2 | Fold 3 | Fold 4 | Fold 5
Split 1
Split 2
Split 3
Split 4
Split 5
Training data
Testing data
[JH15]
Notes: Procedure of five-fold cross validation (CV). The training set in each CV trial consisted of 80% of all samples randomly drawn from the dataset representing 16 cells, while the remaining 20% of the samples were used to form the validation set.

## Slide 85: Hyperparameter tuning
Figure 5.6
[BB12]
Grid search
Random search

## Slide 86: Different concepts of single task learning and multitask learning
Single task learning
Training data
Trained model
Training
Task 1
Prediction 1
Training data
Trained model
Training
Task 2
Prediction 2
Training data
Trained model
Training
Task k
Prediction k
Training data
Task 1
Prediction 1
Training data
Trained model
Joint training
with shared
representation
Task 2
Prediction 2
Training data
Task k
Prediction k
Multitask learning
…
…
…
Figure 5.7
[Car93]
Notes: Difference between multitask learning and traditional single task learning. In MTL the learning process involves all the tasks and is performed jointly, allowing the exchange of information.

## Slide 87: One perceptron of the layer
Figure 5.8
…
Perceptron
[JZL18]
Notes: The circle describes the perceptron, in which is applied the linear combination and the activation function.

## Slide 88
Stucture of deep neural network (DNN)
Input layer
Hidden layer 1
Hidden layer 2
Output layer
Input data
Output result
Figure 5.9
[Saz06]

## Slide 89: Difference between momentum update and Nesterov momentum update
[SMD13]
Figure 5.10
Momentum update
Nesterov momentum update

## Slide 90: Fundamental approach of transfer learning
Source domain
Source task
Target domain
Knowledge
Learning system
Target task
Transfer
Knowledge
Figure 6.1
[OBL14]

## Slide 91: Categorization of transfer learning approaches
Transfer Learning
Inductive Transfer Learning
Transductive Transfer Learning
Unsupervised Transfer Learning
Labeled data are available in a target domain
Labeled data are available only in a source domain
No labeled data in both source and targt domain
Labeled data are available in a source domain
Multi-task Learning
Single domain and single task
Different domains but single task
Domain Adaption
Sample Selection Bias/Covariance Shift
No labeled data in a source domain
Self-taught Learning
[ZLO17]
Figure 6.2

## Slide 92: Distinction between transfer learning and multi-task learning
Transfer learning
Multitask learning
Source task
Target task
Task 1
Task 3
Task 2
Task 4
Figure 6.3
[TS09]
Notes: In transfer learning the information flows in one direction only, from the source task to the target task. In multitask learning, information can flow freely among all tasks

## Slide 93: Component dimensions of the 42 toy building block
Length
Height
Width
Roundness (Rmax-Rmin)
W°
Angular
Figure 7.1

## Slide 94: Qualitative depiction of 2n-Experiment (n=3) plan including star and center point
Figure 7.2
×Step value
2 ×Step value

## Slide 95: Data visualization of the part weight of the six material classes
Material class [-]
Part weight [g]
Figure 7.3

## Slide 96: Feature importance score ranking for prediction of part weight
Figure 7.4
Chart: Feature importance
| Solid density | Holding pressure | Thermal Conductivity | No Flow Temp | Ejection Temp | P2 | Melt density | N0 - Nu Polynom | Thermal diffusivity | Melt temperature | Melt Volume Rate | Suggested Mold Temp | Minimum Mold Temp | Pm4 | Injection flow rate | Maximum Mold Temp | Ts | Specific Heat | Melt Volume Rate | P3 | Cavity wall temperature | Cooling time | P1 | Pm1 | Pm2
 | 0.21539 | 0.12292 | 0.12057 | 0.1053 | 0.07396 | 0.046311 | 0.044874 | 0.034297 | 0.020239 | 0.01904 | 0.019033 | 0.018274 | 0.016138 | 0.011713 | 0.010976 | 0.010604 | 0.009182 | 0.008208 | 0.007636 | 0.007405 | 0.006941 | 0.006358 | 0.006318 | 0.005196 | 0.004288

## Slide 97: Structure of the deep neural network with transfer learning
Source task
Target task
 |  | …………………….. |  | 
 |  | …………………….. |  | 
 |  | …….. |  | 
 | …….. | 
 |  | …………………….. |  | 
 |  | …………………….. |  | 
 |  | …….. |  | 
 | …….. | 
Input layer
(50 node)
Hidden layer
(50 node)
Hidden layer
(25 node)
Hidden layer
(10 node)
Output layer
(5 node)
Reuse
Figure 8.1

## Slide 98: Prediction result of the base model
Chart: Real value of part weight [g]
Figure 8.2

## Slide 99: Comparison of single task, multitask and ensemble learning
Figure 8.3
Chart: Quality values [-]
| Part weight | Length | Angle | Height | Width
Single task learning | 0.69417 | 0.28043 | 0.26579 | 0.2172 | 0.27213
Multitask learning | 2.0714 | 0.28674 | 0.35056 | 0.27839 | 0.52729
Ensemble learning | 0.79228 | 0.26824 | 0.26091 | 0.26259 | 0.31598

## Slide 100: Splitting source task into 5 folds for pre-training DNN models
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX | APEC
Total dataset
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX
Source task
APEC
Target task
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX
PLEXIGLAS | SABIC | ULTEM | ULTRAMID | VALOX
Pre-trained DNN 1
Pre-trained DNN 2
Pre-trained DNN 3
Pre-trained DNN 4
Pre-trained DNN 5
Figure 8.4

## Slide 101: Model structure of transfer learning with ensemble learning
DNN with
transfer learning
(Target: APEC)
Input
Pre-trained DNN
Output of DNN-TL
Material properties
Machine setting parameters
…
…
SABIC
VALOX
ULTEM
APEC
APEC
APEC
Fine tuned DNN
Fine tuned DNN
Fine tuned DNN
…
Mean prediction
Quality value
Ensemble learning
Result
Figure 8.5

## Slide 102: Model comparison of R2 value
Figure 8.6
Algorithms [-]
Chart: 𝑅2 value [-]
| Decision Tree | Random Forest | Gradient Boosting | Ada Boost | Extra Trees | XGBoost | Base DNN | Optimised DNN | DNN-EL | DNN-TL | DNN-ETL
 | 0.7339 | 0.6243 | 0.8287 | 0.6767 | 0.509 | 0.848 | 0.8707 | 0.9071 | 0.8336 | 0.8934 | 0.9115

## Slide 103
Source task
Input A
Target task
Input B
Input B
Input B
Output A
Output B
Self Transfer
Transfer
Learning
Base A
Base B
B2B (Frozen weight)
B2B+ (Fine tuning)
A2B (Frozen weight)
A2B+ (Fine tuning)
Figure 9.1
Overview of the experimental treatments and controls

## Slide 104: Difference of AnB and AnB+ transfer learning model
Figure 9.2
Large dataset
Relatively
small dataset
Input A
Task A
Input B
Task B
Layer n
Back propagation
Back propagation
AnB: Frozen weights
AnB+: Fine tuning
Transfer
Forward direction

## Slide 105: Effect of the number of transferred layers on transfer learning
Chart: Layer n at which network is chopped and retrained [-]
| 0 | 1 | 2 | 3 | 4
Self transfer fine tuning BnB+ | 0.92209 | 0.92861 | 0.92433 | 0.93195 | 0.91819
Self transfer frozen BnB | 0.92209 | 0.9257 | 0.84166 | 0.93732 | 0.92411
Transfer fine tuning AnB+ | 0.92209 | 0.93795 | 0.95449 | 0.96048 | 0.96583
Transfer frozen AnB | 0.92209 | 0.88886 | 0.95946 | 0.95579 | 0.96183
No transfer base B | 0.92209 | 0.92209 | 0.92209 | 0.92209 | 0.92209
Figure 9.3

## Slide 106: Effect of the training dataset size on transfer learning
Figure 9.4
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
No transfer learning | 0.70558 | 0.8874 | 0.92225 | 0.91953 | 0.93167 | 0.90571 | 0.9076 | 0.90784 | 0.92487 | 0.92267
Transfer learning fine tuning | 0.98762 | 0.98211 | 0.98937 | 0.98696 | 0.98087 | 0.99092 | 0.98997 | 0.97923 | 0.98578 | 0.98557
Transfer learning frozen weights | 0.71115 | 0.92785 | 0.95329 | 0.96469 | 0.96794 | 0.97234 | 0.96831 | 0.97528 | 0.96789 | 0.98472

## Slide 107: Different part weight distribution of six material classes
Chart: Part weight [g]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Transfer on 2 sources | -0.65786 | 0.78867 | 0.91295 | 0.93855 | 0.93473 | 0.95444 | 0.947 | 0.96466 | 0.96437 | 0.97572
Transfer on 3 sources | 0.26902 | 0.65035 | 0.90728 | 0.91638 | 0.93412 | 0.9629 | 0.96164 | 0.95907 | 0.97552 | 0.97603
45 50 55 60 65 70 75
APEC
PLEXIGLAS
SABIC PP
ULTEM
ULTRAMID
VALOX
Figure 9.5

## Slide 108: Effect of the number of source datasets on transfer learning
Chart: Percentage of training set [%]
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Transfer on 1 source | -0.47718 | 0.76524 | 0.86788 | 0.91091 | 0.88879 | 0.93419 | 0.94236 | 0.96013 | 0.96468 | 0.95642
Transfer on 2 sources | -0.65786 | 0.78867 | 0.91295 | 0.93855 | 0.93473 | 0.95444 | 0.947 | 0.96466 | 0.96437 | 0.97572
Transfer on 3 sources | 0.26902 | 0.65035 | 0.90728 | 0.91638 | 0.93412 | 0.9629 | 0.96164 | 0.95907 | 0.97552 | 0.97603
Transfer on 4 sources | 0.26925 | 0.75573 | 0.87924 | 0.90247 | 0.9428 | 0.95161 | 0.96635 | 0.9621 | 0.96659 | 0.97443
Transfer on 5 sources | 0.34041 | 0.69868 | 0.86845 | 0.92629 | 0.95951 | 0.97064 | 0.97776 | 0.96976 | 0.96729 | 0.97831
No transfer | -0.34814 | 0.2251 | 0.86542 | 0.9167 | 0.8922 | 0.91901 | 0.9177 | 0.92527 | 0.91701 | 0.92486
Figure 9.6